FAQ七：Problems, Causes and Solutions that may arise during the use of the pu foam.

- it can’t spray out.The pu foam can spray when you shake the can.If there is a situation that can be shaken but cannot spray or spray finished.

- There may be the following reasons：

- ①The foam gun is not installed in place, and the valve is not opened.②The foam gun muzzle, adapter, or barrel is blocked. To clean up immediately, use the foam cleaner can be used to check Whether unobstructed (when unobstructed, the foam cleaner is smooth and powerful); Or directly replace a new foam gun.

- ③The phenomenon of "closing valve" occurs in the pu foam valve,It may be caused by long upside down.Can put down the jar first,after 5 minutes with a 4 * 30 nail insertion of the valve and knock gently with hammer a nail, heard ventilation on gun can immediately after use, suggested immediately once finished.

A bottle of pu foam had better be used up in one time. If it is really not used up and the gun does not leak out, don't unloading the gun and tighten the adjusting screw behind the foam gun, which can be placed for a week.If the air tightness of the gun is not good, the material tank must be removed and the foam gun must be cleaned. The semi-tank product is treated as a "knot valve", but it is possible that the valve resetting is not tight and the valve will be solidified due to air leakage. The non-standard foaming gun may not match the foaming agent parts system, which may cause the valve to not open or fully open,it shows that can't spray foam or out of the foam glue pressure is insufficient. If the detergent solubility is not enough, the foam gun is difficult to clean, spray foam will not be used smoothly.(Shuode company's standard foam gun and cleaner are recommended).

2) shrinkage.There are a lot of customers because of the use of poor quality products, leading to the contraction of high-grade wooden doors, for high-end wooden doors recommended use of wood door special pu foam.(Such as the development and production of Shanghai Shuode DR I DRII,little shrinkage,and strong bonding strength).

3)Spray foam like water.Because the workers in the production process a raw material is missing without expansion, the general probability is very small, In this case, manufacturers will change the goods.